## Slide 1: WETTING AND NON-WETTING
<number>
Avi Marmur
Chemical Engineering Department
Technion – Israel Institute of Technology
Haifa, Israel
Notes: <number>

## Slide 2
<number>
NON-WETTING
In Air
Low Sliding/Roll-Off Angle
Under A Liquid
Stable Air Film

Notes: <number>

## Slide 3: THE LOTUS EFFECT
<number>
Barthlott & Neinhuis (1997) University of Bonn
Notes: <number>

## Slide 4: THE LOTUS EFFECT
<number>
Barthlott & Neinhuis (1997) University of Bonn
Notes: <number>

## Slide 5: SELF-CLEANING SURFACES?
<number>
Notes: <number>

## Slide 6: BIOFOULING PREVENTION?
<number>
Biofouling of a ship hull by barnacles
(photo courtesy International Paint Ltd).
Notes: <number>

## Slide 7: HOW TO INDUCE NON-WETTING?
Minimize Solid-Liquid Contact Area
Minimize Contact Angle Hysteresis
<number>
Need to Understand
Wetting Fundamentals

## Slide 8: MINIMIZE CONTACT AREA
Decrease Solid-Liquid Contact Area
By Increasing the Contact Angle (CA)
<number>
LIQUID
AIR
SOLID



## Slide 9: WETTING ON AN IDEAL SOLID SURFACE
THE YOUNG EQUATION (1805)
<number>
1773-1829
In NatureY < ~120o
SOLID
LIQUID
FLUID

Notes: <number>

## Slide 10: WETTING ON ROUGH SURFACES The Wenzel Equation (1936) for Homogeneous Wetting
<number>

Roughness Ratio =
Actual area
Nominal area
Notes: <number>

## Slide 11: IMPLICATIONS OF THE THE WENZEL EQUATION
<number>
r =
Actual area
Nominal area
Wenzel, R. N. J. Ind. Eng. Chem. 1936, 28, 988
Notes: <number>

## Slide 12: WHEN IS THE WENZEL EQ. CORRECT?
3-d, General Proof
ap  W when drop is -large
An -large drop is symmetrical
Wolansky, G., Marmur, A., Coll. Surf. A 156, 381 (1999).
<number>
Notes: <number>

## Slide 13: Is Wenzel Good Enough for non-wetting?
<number>
Notes: <number>

## Slide 14: A SIMPLE EXAMPLE OF HOMOGENEOUS WETTING
110o 150o requires r ~ 2.5 !
Contact area may not be small enough
<number>
r = 1.5: 110°120°
r = 2: 110°  133°

## Slide 15
<number>
WETTING ON
ROUGH SURFACES
Homogeneous Wetting
Wenzel (1936)
Heterogeneous Wetting
  Chemical heterogeneity
Cassie-Baxter (1944)
Notes: <number>

## Slide 16
<number>
HETROGENEOUS WETTING ON ROUGH SURFACES
Chemical Heterogeneity
Minimization of Contact Area

Notes: <number>

## Slide 17: HETEROGENEOUS WETTING ON SMOOTH SURFACES The Cassie Equation for the Most Stable CA
<number>
Weighted Average of CA Cosines
Cassie, A.B.D., Disc. Faraday Soc. 3, 11 (1948).
Notes: <number>

## Slide 18: THE CASSIE EQUATION IS CORRECT ONLY FOR LARGE DROPS 3-D Simulation
<number>
Brandon, S., Haimovich, N., Yeger, E., and Marmur, A.,
J. Coll. Int. Sci. 263, 237-243 (2003)
Notes: <number>

## Slide 19: THE CASSIE-BAXTER (CB) EQ. Heterogeneous Wetting: Air Pockets
<number>
f – fraction of projected wet area: 0  f  1
rf ( f ) – local roughness ratio
(1-f) – fraction of entrapped air in pores
Y
f
rf

Notes: <number>

## Slide 20: WETTED AREA (Lotus Leaf Simple Model)
<number>
ACB < AW
For the same CA
A - wetted area
Notes: <number>

## Slide 21: TRANSITION BETWEEN WENZEL AND CB
<number>
Johnson & Dettre, Adv. In Chemistry Series 43, ACS, Washington, D.C. 1964
Stability vs. Metastability
  The lower angle - stable
Dependence on r only?
Notes: <number>

## Slide 22: TRANSITION BETWEEN WENZEL AND CB
<number>
Wenzel & Cassie-Baxter theories predict CA corresponding to the global minimum of the free energy
Johnson & Dettre predicted
- many metastable configurations and the actual CA can differ from one corresponding to the global minimum one
- the heigths of the energy barriere are app. directly proportional to the heigth of aspirities
a sharp transition from Wenzel to Cassie-Baxter regime with increasing roughness (critical roughness)
CA hysteresis  until the critical roughness reached, then 
Notes: <number>

## Slide 23: TO BE HETEROGENEOUS OR NOT TO BE?
<number>
Local Minima of G*(f, 
CB EQUATION
f – fraction of projected wet area
rf ( f ) – local roughness ratio
(1-f) – fraction of entrapped air in pores

Y
f
rf
Notes: <number>

## Slide 24: TO BE HETEROGENEOUS OR NOT TO BE?
<number>
AC – B2 > 0
d2(rf f )/df 2 > 0
Overrides CB
Marmur, A. Langmuir 19, 8343-8348 (2003)
Dependence on specific topography!
Feasibility Condition
Notes: <number>

## Slide 25: Minimize CA Hysteresis?
<number>
Notes: <number>

## Slide 26: REAL SURFACES: CA HYSTERESIS Experimental Observations
<number>
Multiple CAs
Advancing CA
Stick-Slip
Receding CA
Notes: <number>

## Slide 27: GIBBS ENERGY ON REAL SURFACES
<number>
Multiple Minima
Metastable & Stable CAs
Energy Barriers
Theoretical & Practical ACA and RCA
TRCA
PRCA
Global
Minimum
Energy
Barrier
PACA
TACA
Metastable
Equilibrium
Notes: <number>

## Slide 28: SLIDING ON A TILTED PLANE
<number>
max
min
min and max differ
Hysteresis prevents sliding
Krasovitski & Marmur, Langmuir 1, 3881-3885 (2005)
Notes: <number>

## Slide 29: MINIMIZE CA HYSTERESIS
Two Ways:
Produce Ideal Surfaces (not Practical)
Induce Heterogeneous Wetting (Air!)
<number>

## Slide 30: PRACTICAL CONCLUSION
Min contactArea Min hysteresis
Heterogeneous Wetting (CB)
<number>
